Reviewer Notes:  Please make appropriate changes based on the pile type on your job.

GALVANIZED (STRUCTURAL STEEL)(CAST-IN-PLACE CONCRETE) PILE AND BRACING	1/03/17

1.0  Description.  This job special provision contains general requirements for furnishing, coating and placing galvanized steel piles and bracing as shown on the plans and shall be in addition to the requirements of Sec 702.

2.0  Material.  Structural steel piles and bracing shall be galvanized in accordance with ASTM A123 and Sec 1080.  Repairs to the galvanized coating and field galvanizing shall be in accordance with ASTM A780.  Zinc rich paints will not be allowed.  Repairs and field galvanizing will not be required where the pile will be encased in concrete or below the limits specified in section 3.0 of this job special provision.  Protective Coatings specified in Sec 702 will not be required for galvanized piles or bracing.

3.0  Construction Requirements.

3.1  Galvanizing material shall be omitted or removed 1 inch clear of weld locations.  The method used to omit or remove the galvanizing material shall be masking, grinding or other methods as approved by the engineer.  If a weld location falls within an area where galvanizing is required, clean the weld area making sure to remove all welding slag.  Then field galvanize the weld area in accordance with ASTM A780.  Zinc rich paints will not be allowed.

3.2  All pile below the pile concrete encasement shall be galvanized down to an elevation as shown on the plans.

3.3  At the contractor’s option, the entire pile length may be galvanized.

4.0  Method of Measurement.  Galvanized (Structural Steel)(Cast-In-Place Concrete) Pile in place will be the actual length to the nearest linear foot for that portion of the pile that remains permanently in the structure.  See Sec 702 Basis of Payment for any additional length authorized by the engineer resulting from pile splices.  No separate measurement will be made for pile that is not galvanized.  Measurement of bracing as Galvanized Fabricated Structural Carbon Steel (Misc.) will be based on the plan quantities.

5.0  Basis of Payment.  The accepted quantity of galvanized and non galvanized pile in place will be paid for at the contract unit price for Galvanized (Structural Steel)(Cast-In-Place Concrete) Pile.  No direct payment will be made for incidental items necessary to complete the work unless specifically provided as a pay item in the contract.  Galvanized pile bracing in place will be paid for at the contract unit price for Galvanized Fabricated Structural Carbon Steel (Misc.).