Use this BSP when directed to by the Environmental Section on larger paint projects. Items in red will need to be updated for your particular bridge.

PAINT REMOVAL						4/17/18

- Heavy Metal Paint Removal (blast media recycler allowed).  Based on MoDOT’s screening results, the paint on bridge # XXXX may exceed the heavy metal regulatory limits for heavy metal constituents (lead & barium). All paint removal shall use steel grit as the approved blast media; spent paint waste/blast media shall be managed as non-hazardous blast residue and shipped to Doe Run smelter for use in their smelting process.  Shipping labels shall be provided to the contractor by MoDOT’s Environmental section.

- Pursuant to 10 CSR 25.9.020 (2) (B), if solvent recycling/recovery activities are used as a part of the operation, the contractor shall notify the Missouri Department of Natural Resources (MDNR) of their exempt status from the resource recovery certification requirements.  The notification shall be made to MDNR, Hazardous Waste Program, P.O. Box 176 Jefferson City, MO 65102.  This notification shall identify the owner and operator, the name and location of the facility, identification of the waste(s) recovered, method(s) of recovery, and the approximate monthly quantity of waste recovered.  This notification shall be made to MDNR prior to starting work, and it shall also be provided to the Engineer. When using a solvent recovery system, the site can generally be managed as a small quantity generator (SQG) of hazardous waste.

- If solvent/paint waste generation results in the generation of hazardous waste quantities exceeding 2,200 pounds per month (i.e., generally greater than 4 drums of solvent/paint waste) the site shall be managed as a large quantity generator (LQG) of hazardous waste.  Contractor responsibilities as a LQG are outlined in the Missouri Standard Specifications for Highway Construction in sections 1081.4.3.1 – 1081.4.3.3.5 and 107.1.  The specific LQG requirements can be referenced in 40 CFR Part 262 and 10 CSR 25.  Note: Management of all waste streams generated on site as a part of site operations is a LQG requirement (i.e., paint chips, solvent cake, PPE, towels/wipes, batteries, wash water, water from compressors, used oil, and universal waste).

- The contractor requirements for management of a LQG site will be discussed at the pre-construction conference.  The applicable LQG contractor requirements are outlined in MDNR’s Large Quantity Generator Inspection Checklist at the following link:  http://dnr.mo.gov/forms/780-1525-f.pdf

- If the operation qualifies as a LQG site, the contractor shall ensure that all pertinent personnel working on site meet the training requirements as defined in 40 CFR 265.16 (personnel training).  LQG regulation also requires that the operation maintains a contingency plan on site as defined in 10 CSR 25-5.262(1) incorporating 40 CFR 262.34(a)(4) referencing 40 CFR 265.53(a).

- If hazardous waste generation exceeds 220 pounds per month, the contractor shall be responsible for registering the site and procuring the EPA and Missouri ID numbers. Sample collection and laboratory analysis of spent solvent will be the responsibility of the contractor to properly characterize the material, and make an accurate hazardous waste determination. If the material is determined to be hazardous waste, it shall remain stored on site until transport for disposal to an EPA-approved treatment, storage or disposal (TSD) facility by a licensed hazardous waste transporter.  No transport of the hazardous waste off site via roadway for temporary storage shall be allowed.

- If the site requires registration as either a SQG or LQG, the contractor shall be responsible for all necessary reporting (i.e., submitting quarterly, annual, and/or biennial reports to Missouri DNR and EPA as required by regulation).  Deactivation of the site registration will be the responsibility of the contractor.  Completed copies of all forms, manifests, and reports will be submitted to the Engineer.

- Fees and taxes will be the responsibility of the contractor.

2.0  Method of Measurement.  No measurement will be made.

3.0  Basis of Payment.  Payment for the above described work, including all material, equipment, labor and any other incidental work necessary to complete this item, will be considered completely covered by the contract unit price for Surface Preparation for Recoating Structural Steel.