## Slide 1: Superpave Homework Review
09/10/2021

## Slide 3: Module 1 Introduction to Superpave Homework
Question # 1.
What 4 types of pavement distress are minimized when mixes are designed in accordance with Superpave criteria?

## Slide 4: Answer - M1-Q1; (slide 5)
Permanent Distortion
Fatigue Cracking
Cold Temperature Cracking
Moisture Sensitivity (Stripping)

## Slide 5: Module 1
2. Where are guidelines for testing and inspection of MoDOT projects found?

## Slide 6: Answer - M1-Q2; (slide 71)
EPG guidelines
Task Force (FAQ) guidelines

## Slide 7: Module 1
3. What is the 403 target for air-voids for an SP250 mix?
Answer (Slide 74): Va = 4 ± 1.0%

## Slide 8: Module 1
4. What is the 403 - field tolerance for VMA?
Answer (Slide 74) :
VMA Design Minimum is - 0.5 to 2.0%
ENLARGED

## Slide 9: Module 2 Mix Design Overview Mix Design/Pavement Structure Design
1. For an SP125B mix, what is the design traffic level in ESALS?

## Slide 10: Answer - M2- Q1; (slide 22)
SP125B mix
≥ 30,000,000

## Slide 11: Module 2
2. What specifications cover Superpave mixes for Hot Mix and for Aggregate?

## Slide 12: Answer - M2 - Q2; (slides 6 and 11)
1002 and 403 Superpave
NOTE:
SPECS = Specifications

## Slide 13: Module 2B Mix Design Overview - Aggregate Quality
1. For SP125B mix, during the design phase, what is the minimum (or maximum, or acceptable range) acceptance level for the following:
a. Fractured face count (CAA)
b. Fine Aggregate shape (FAA)
c. Sand Equivalent (SE)
d. Flat and Elongated (F & E)

## Slide 14: Answer - M2B - Q1; (slides 19)
NOTES:
CAA = Coarse Aggregate
FAA = Fine Aggregate
SE = Sand Equivalent
F&E = Flat & Elongated
a. Fractured face Count = 100/100
b. Fine Aggregate Particle Shape = 45
c. Sand Equivalent = 50
d. Flat and Elongated = 10

## Slide 15: Module 2C Mix Design Overview - Binder, Rap, & Shingles
1. For a 70-28, what do the number signify?

## Slide 16: Answer - M2C - Q2; (slides 9)
NOTES:
PG= Performance Grade
70 = Rut Resistant up to 70°C
-28 = Cold temperature cracking resistant down to -28°C

## Slide 17: Module 2C
2. For the following M320 binder grades, what are the ~ equivalent M322 grades?

## Slide 18: Answer - M2C - Q2; (slides 63)
NOTE:
S = Standard Traffic
H = Heavy Traffic
V = Very Heavy Traffic
M320 | M332
PG 64-22 | 64-22 Grade S
PG 70-22 | 64-22 Grade H
PG - 76-22 | 64-22 Grade V

## Slide 19: Module 2C
3. What is the major extra test in M322 compared to M320?

## Slide 20: Answer - M2C - Q3; (slides 62)
MSCR Test
Multiple Stress Creep Recovery
NOTE:
Asphalt binder is tested on a DSR Instrument.
DSR = Dynamic Shear Rheometer

## Slide 21: Module 2C
4. For a mix containing RAP, what materials may be in the IN-LINE binder grade compared to the contract grade?
NOTE:
RAP = Recycled Asphalt Product
A rejuvenator will most likely be used to
revive the aged binder of RAP. In addition, because the binder is aged it will grade high on a DSR machine, so the RAP will be mixed with a soft virgin binder, like a PG 58 – 22 to bring the grade down.
Virgin Binder : Is a binder that has NO additives or modifiers in it, sometimes it is also called a NEAT BINDER or NEAT ASPHALT.

## Slide 22: Answer - M2C - Q3; (slides 82)
Soft Virgin Binder
Additives/Modifiers/Rejuvenators

## Slide 23: Module 2D Mix Design Overview Volumetrics
1. For an SP125B mix, during the design phase, what is the minimum or acceptable range) for:
a. Air-voids
b. VMA
c. VFA

## Slide 24
Answer -

## Slide 25: Module 2D
2. Calculate the combined (weighted average) Gsb of the aggregate blend shown on the attached JMF.
NOTE:
JMF = Job Mix Formula

## Slide 26
Job Mix Formula

## Slide 27: Answer - M2D - Q2; (Slide 73)

## Slide 28: Module 2D
3. What 2 things occupy the space in VMA?
VMA =
Air Voids + Effective Asphalt
ANSWER(SLIDE 9):

## Slide 29: Module 2D
Total binder content has 2 portions.
What are they?
Total Binder Content =
Absorbed Binder + Effective Binder
ANSWER (SLIDE 12):

## Slide 30: Module 2D
5. Describe what VFA represents?
ANSWER (SLIDE 18):
% of VMA filled with effective asphalt.

## Slide 31: Module 2D
6. In general, what 5 things can be done to increase VMA?
ANSWER (SLIDE 54):

## Slide 32: Module 2D
7. What 2 tests are used to determine Bulk Specific Gravity of aggregate?

## Slide 33: Answer - M2D - Q7; (slide 65)
1. T84
(Specific gravity of fine Aggregate)
2. T85
(Specific gravity of Coarse Aggregate).

## Slide 34: Module 2D
8. What test is used to determine Effective Specific Gravity of aggregate?
T209 – Rice - Specific Gravity - Gmm
ANSWER (SLIDE 81):

## Slide 35: Module 2E and 2F Mix Design Overview - Mix Design Phase 1 & 2
1. During the design phase, for an SP125B mix, what are the required number of gyrations for Nini, Ndes, and Nmax?

## Slide 36: Answer - M 2E and 2F - Q1; (slide 35)
Nini = 9
Ndes = 125
Nmax = 205

## Slide 37: Module 2E and 2F
2. During the design phase, for an SP125B mix, what are the required compaction levels (%Gmm) for Nini, Ndes, and Nmax?

## Slide 38: Answer - M 2E and 2F - Q2; (slide 50)
Nini : ≤ 89.0
Ndes: 96.0
Nmax: ≤ 98.0

## Slide 39: Module 2E and 2F
3. Phase 1 is to determine design gradation or final binder content?
Gradation
ANSWER (SLIDE 3):

## Slide 40: Module 2E and 2F
4. Phase 2 is to determine gradation or final binder content?
ANSWER (SLIDE 46):
Final binder content

## Slide 41: Module 2G Mix Design Overview: TSR JMF & Field verification Miscellaneous
1. What 9 pieces of information on the JUM can be useful to the QC or QA?

## Slide 42: Answer – m2G; (slide 46)

## Slide 43: Module 3 Plant Operations - Gradation
1. For QC; What is the minimum sampling frequency for gradation samples at the HMA plant?
Should they retain a split?

## Slide 44: Answer - M3 - Q1; (slide 70)
1 per 2 sublots
Yes, they should retain a split.

## Slide 45: Module 3
2. For an SP250B mix, given the following QC, sample’s gradation off the cold feed at a drum mix plant, what specifications (with tolerances applied) should the sample meet?
Did the gradation pass?

## Slide 46: Answer - M3 – Q2; (slide 80)
NO, Failed on #200 sieve.

## Slide 47: Module 3
3. For QA: What is the minimum sampling frequency for the independent gradation samples at the HMA plant?
1 per 4 Sublots
ANSWER (SLIDE 71):

## Slide 48: Module 3
4. What is QA’s minimum testing frequency for the QC retained splits for gradation samples at the plant?
ANSWER (SLIDE 71):
1 Per week minimum

## Slide 49: Module 3
5. When comparing QA to QC gradations from retained splits, what is considered “Favorable comparison”?

## Slide 50: Answer - M3 – Q5; (slide 95)

## Slide 51: Module 3 - Plant Operations - Consensus Tests
6. For QC, what is the minimum sampling frequency for consensus test samples at the HMA plant for QC?
Should they retain a split?

## Slide 52: Answer - M3 – Q6; (slide 70)
1 per 10,000 TONS
1 per project per mix type
YES, retain a split

## Slide 53: Module 3 - Plant Operations - Consensus Tests
7. For QC: For an SP250B mix, what are the allowable limits (Specification with field tolerances applied) for consensus test values? Given the following QC consensus test results, did the sample pass?

## Slide 54: Answer - M3 – Q6; (slide 70)
No,
SE Sand Equilivent Test Failed

## Slide 55: Module 3 - Plant Operations - Consensus Tests
8. For QA: What is the minimum sampling frequency for independent QA consensus test samples at the HMA plant?

## Slide 56: Answer - M3 – Q7; (slide 71)
1 per project per mix type
No matter how many mixes.

## Slide 57: Module 3 - Plant Operations - Consensus Tests
9. For QA: What is QA’s minimum testing frequency for the QC retained splits for consensus test samples at the HMA plant?

## Slide 58: Answer - M3 – Q9; (slide 71)
1 per project minimum.
(no matter how many mixes)

## Slide 59: Module 3 - Plant Operations - Consensus Tests
10. When comparing QA to QC consensus test results from retained splits, what is considered “favorable comparison”? Given the following, is there a “favorable comparison”?

## Slide 60: Answer - M3 – Q10; (slide 92)
YES, favorable comparison on all four tests.

## Slide 61: Module 3 - Plant Operations - Consensus Tests
Where should the consensus
sample be taken?
Cold Feed Belt
ANSWER (SLIDE 71):

## Slide 62: Module 3 - Plant Operations - Deleterious Material
12. For QC: what is the minimum sampling frequency for QC deleterious material samples at the HMA plant?

## Slide 63: Answer - M3 – Q12; (slide 70)
1 per 2 Sublots

## Slide 64: Module 3 - Plant Operations - Deleterious Material
13. For QA: What is the minimum sampling frequency for independent QA deleterious material test samples at the HMA plant?

## Slide 65: Answer - M3 – Q13; (slide 71)
1 per 4 Sublots

## Slide 66: Module 3 - Plant Operations - Deleterious Material
14. Where should the deleterious sample for aggregate be taken?
All plants – Cold feed belt
ANSWER (SLIDE 71):

## Slide 67: Module 3 - Plant Operations - General
15. What does MoDOT do on an annual basis at the quarry?

## Slide 68: Answer - M3 – Q14; (slide 55)

## Slide 69: Module 4 QC/QA Overview and Hot Mix Asphalt quality Control Plan
1. In the QC plan short form, what information is required about lots and sublots?

## Slide 70: Answer - M4 – Q1; (slide 15)
Lot and Sublot sizes and how they will be designated.

## Slide 71: Module 4
2. In the QC plan short form, what information is required about binder content testing?
Binder Content Test Method
ANSWER (SLIDE 15):

## Slide 72: Module 4
3. In the QC plan short form, what information is required about coring?
Number of cores cut per sample
ANSWER (SLIDE 15):

## Slide 73: Module 4
4. What is a very critical item in the agreement between the HMA producer and the aggregate producer?
ANSWER (SLIDE 5):

## Slide 74: Module 4
5. In the QC plan short form, what information is required about the gradation sample?
Whether gradations will
be on T308 residue.
ANSWER (SLIDE 15):

## Slide 75: Module 5 Sampling Loose Mix and Cores
1. For routine lots, are there requirements for lot size under the 403 specification contracts?

## Slide 76: Answer - M5 – Q1; (slide 6)
No Specified Limitation.

## Slide 77: Module 5
2. What are the minimum number of sublots per lot?
4 sublots per lot.
ANSWER (SLIDE 7):

## Slide 78: Module 5
3. What is the maximum sublot size?
1,000 TONS.
ANSWER (SLIDE 7):

## Slide 79: Module 5
4. Are non-integral shoulders included in the traveled way lot routine?
NO
ANSWER (SLIDE 8):

## Slide 80: Module 5 – For Volumetrics / Binder content loose mix samples:
1. For QC: What is the frequency of sampling for QLA analysis?
Is a retained sample required?
Should the location be random?

## Slide 81: Answer - M5 – Q1; (slide 16)
One per Sublot
Yes,
A retained sample is required.
Yes,
The location should be random.

## Slide 82: Module 5 - For Volumetrics / Binder content loose mix samples:
2. For QA: Who should obtain the independent QA QLA loose mix sample QA or QC?
At what minimum frequency?
Is a retained sample required?
Should the location be random?
NOTE:
QLA = Quality Level Analysis

## Slide 83: Answer - M5 – Q2;
(Slide 26) Who? Independent QA QLA. QA or QC? QA
(Slide 18) At what minimum frequency? One per 4 sublots
(Slide 19) Is a retained sample required? Yes
(Slide 21) Should the location be random? Yes

## Slide 84
3. List the steps in the sample quartering process.
Module 5 - For Volumetrics / Binder content loose mix samples:

## Slide 85: Answer - M5 – Q3; (slide 60 & 75)
1. Mix, avoid segregation.
Split/Quarter.
Combine & retain opposite quarter
(50 lbs.).
Combine other
two quarters (50 lbs.).

## Slide 86
4. For QA: What is the minimum testing frequency of the QC retained sample?
Module 5 - For Volumetrics / Binder content loose mix samples:

## Slide 87: Answer - M5 – Q4; (slide 18)
One per day

## Slide 88
5. N/A? NOTE: Avoid heating above molding temperature
6. What are check samples used for?
Module 5 - For Volumetrics / Binder content loose mix samples:

## Slide 89: Answer - M5 – Q6; (slide 11)
* Check how the mix is doing
* Investigate problems
* Determine Limits of the problem
NOTE:
QLA = Quality Level Analysis

## Slide 90
7. In order for a check sample to be used for defining removal limits, what information must be tied to it?
* Gyro pucks
* Gyration/height printouts
* Binder content printouts
ANSWER (SLIDE 15):
Module 5 - For Volumetrics / Binder content loose mix samples:

## Slide 91: Module 5 - For Volumetrics/Binder content loose mix samples.
ANSWER (SLIDE 11):

## Slide 92: Module 5 – For TSR loose mix samples:
1. What is the frequency of sampling QC?
One per 10,000 TONS
ANSWER (SLIDE 22):

## Slide 93: Module 5 – For TSR Loose Mix Sample
2. For QA: Who should obtain the independent QA loose mix sample QC or QA?
At what minimum frequency should the sample be taken?

## Slide 94: Answer - M5 – Q2; (slide 22)
QA obtains the independent
loose mix sample.
QA = One per 50,000 TONS
or
Minimum 1 per combination of
projects.

## Slide 95: Module 5 – For TSR Loose Mix Sample
3. List the steps in the TSR sample quartering process.

## Slide 96: Answer - M5 – Q3; (slide 88, 89, 90)

## Slide 97: Module 5 – For TSR Loose Mix Sample
4. What locations are allowable for TSR samples?

## Slide 98: Answer - M5 – Q4; (slide 21,22)
Random Sample Locations.
Roadway, Plant Discharge
and Truck.

## Slide 99: Module 5 – For TSR loose mix samples:
5. Should QA get their sample at the same location?
ANSWER (SLIDE 23):
Yes, but not at the same time.

## Slide 100: Module 5 – cores from the traveled way:
1. Does QA obtain an independent core?
Yes
ANSWER (SLIDE 103):

## Slide 101: Module 5 – cores from the traveled way
2. What is the minimum QA witnessing/testing frequency for cores?
1 sample per 4 sublots.
ANSWER (SLIDE 103):

## Slide 102: Module 5 – Cores from the traveled way:
3. What is the minimum QC Sampling and testing frequency for core samples?
1 sample per sublot.
ANSWER (SLIDE 103):

## Slide 103
4. What is meant by a core “sample”?
Module 5 –
Cores from the traveled way:
ONE CORE
ANSWER (SLIDE 103):

## Slide 104: Module 5 – cores from unconfined longitudinal joints:
1. What is the sampling frequency?
ANSWER (Slide 116)
QC 1 per Sublot, QA 1 per Sublot
Module 5 – cores from non-integral shoulders:
1. What is the sampling frequency?
ANSWER (Slide 116)
QC 1 per Sublot, QA 1 per Sublot

## Slide 105: Module 5 – sampling points homework:
1. For a 3,000 ton lot, divide into 4 sublots and determine at what tonnage the loose mix samples should be taken, and at what roadway offset. The roadway is 12ft wide, with no unconfined joints. For random numbers, use the table in Module 5: column 3, starting with number set 11 (from the top). Choose 4 pairs (A and B) of numbers moving down the column.

## Slide 107
MODULE 5 – PROBLEM 1
NOTE: 3,000/4 = 750 TONS
Use Regular Rounding

## Slide 108
MODULE 5 – PROBLEM 1
Use Regular Rounding

## Slide 109: Module 5 – sampling points homework:
2. For the same lot, determine the sampling points for all QC cores in the lot. 1100 + 00. The sublot ending stations are 1050 + 50, 1100 + 50, 1149 + 00, and 1199 + 10. The roadway width is 12ft. For random numbers, use column 4, starting with number set 6 (from the top). Choose 4 pairs (A and B) of numbers moving down the column.

## Slide 111
MODULE 5 – PROBLEM 2
ANSWER -
Use Regular Rounding

## Slide 112
MODULE 5 – PROBLEM 2
ANSWER -
Use Regular Rounding

## Slide 113: Module 6 Gyratory Compactor Operations AASHTO T312
What height should the volumetrics gyro pucks be compacted to at the end of the prescribed number of gyrations?
How about the TSR pucks?

## Slide 114: Answer - M6 – Q1; (slide 17)
Volumetrics pucks: 115 ± 5 mm
TSR pucks: 95± 5 mm

## Slide 115: Module 6
2. What is the difference between gyro verification and calibration?
NOTE: Gyro = Gyratory Compactor

## Slide 116: Answer - M6 – Q2; (slides 70, 81,77)
Verification:
Verifies if the calibration is still in spec.
No adjustments made
Uses external angle
Shorter version
Calibration:
Calibrates the gyro.
Adjustments can be made to bring the gyro in spec.
Uses internal angle
Full calibration – takes longer to do.
Note: Extra information added by Donna

## Slide 117: Module 6
3. How often should gyro verification be performed and in what condition should the gyro be in?
NOTE: Gyro = Gyratory Compactor

## Slide 118: Answer - M6 – Q3; (slide 77)

## Slide 119: Module 6
4. How often should calibration be performed on the Gyratory?
ANSWER (SLIDE 66):

## Slide 120: Module 6
What five things do
you check during gyro verification?
ANSWER (SLIDE 76):

## Slide 121: Module 6
6. During field verification of mix volumetric properties, specimens should be compacted to which number of gyrations: Nini, Ndes, or Nmax?
Ndes
ANSWER (SLIDE 32):

## Slide 122: Module 6
7. During field verification of mix volumetric properties, what do you use the gyro-compacted puck data (Gmb) for?
Gmb is not only used to calculate volumetric properties, but also used for Tenderness potential (density), and Moisture sensitivity, (TSR).
ANSWER (SLIDE 9):

## Slide 123: Module 6
8. Where do you obtain the specimen weight for volumetric gyro pucks??
ANSWER (SLIDE 16):

## Slide 124: Module 6
9. Is the required TSR puck weight different from the volumetric gyro puck weight?
Yes
ANSWER (SLIDE 124):

## Slide 125: Module 6
10. Calibration is to be of which angle, internal or external?
Internal
ANSWER (SLIDE 70):

## Slide 126: Module 6
11. The internal calibration angle should be?
1.16 ± 0.02°
ANSWER (SLIDE 70):

## Slide 127: Module 6
12. How is angle verification handled?
The external angle verified monthly during production; it must correspond to be within the proper internal angle range as established during calibration.
ANSWER (SLIDES 80 and 81):

## Slide 128: Module 6
13. How often should the critical mold dimensions be checked?
Minimum of 12 months
ANSWER (SLIDE 86):

## Slide 129: Module 7 Maximum specific Gravity of Voidless loose mix (rice) - Gmm
On the accompanying data sheets, calculate Gmm of the loose mix, Gmb of the compacted gyro puck, and the volumetrics: air voids (Va), VMA and VFA.
- Re-calculate Gmm if the dry-back procedure is used, and the new surface dry weight (A2) is 1574.4g.

## Slide 130
ANSWER – M7 – Q1; (SLIDE 103)
Use Regular Rounding

## Slide 131
ANSWER – M7 – Q1; (SLIDE 103)
Use Regular Rounding

## Slide 132
ANSWER – M7 – Q1; (SLIDE 103)
DRY BACK
Use Regular Rounding

## Slide 133
ANSWER – M7 – Q1; (SLIDE 103)
DRY BACK
Use Regular Rounding

## Slide 134: Module 7
2. Of what use is Rice gravity (Gmm) data?
Compute air voids and
to Compute Pavement density
ANSWER (SLIDE 6):

## Slide 135: Module 7
3. What should be the air void content of a Rice Specific Gravity Specimen?
Zero
ANSWER (SLIDE NA):

## Slide 136: Module 7
4. Where do you obtain the Rice sample?
Behind a paver,
TSR sample,
Truck,
Roadway, Plant
ANSWER (SLIDE 5):

## Slide 137: Module 7
5. What are the 2 ways of verifying that the moisture content in the Rice specimen is below the maximum allowed?
Dry specimen to constant mass
or
Run AASHTO T329
ANSWER (SLIDE 10):

## Slide 138: Module 7
6. Under what condition do you employ the “dry-back” procedure?
When the absorption is > 2%
ANSWER (SLIDE 20):

## Slide 139: Module 7
7. What are the minimum required sample sizes for the following?
a. SP125 -
b. SP190 -
c. SP250 -

## Slide 140: Answer – M7 – Q7; M5, slide 75 Quartering Loose Mix Step 5

## Slide 141: Module 7
8. Why do you crumble the Rice gravity specimen?
To eliminate air from the sample
ANSWER (no SLIDE):

## Slide 142: Module 7
9. Why do you shake the
rice gravity specimen?
To de-air the sample.
ANSWER (SLIDE 28):

## Slide 143: Module 7
10. Why do you pull a vacuum on Rice gravity specimen?
To de-air the sample, to aid in reaching Zero Air-voids.
ANSWER (SLIDE 28):

## Slide 144: Module 7
11. What is the official name of the Rice gravity?
Theoretical Maximum specific Gravity
ANSWER :

## Slide 145: Module 8 Asphalt content ignition oven method t308
1. What is the “aggregate Calibration (or, Correction) Factor” [now called the “Asphalt Binder Correction Factor”]? How is it applied? Who determines it?.
-What:
-How applied:
-Who determines QC or QA?

## Slide 146: Answer – M8 – Q1; (slide 54, 55)
-What: To correct for loss of mass during the mix ignition due to aggregate burn-off.
Who determines QC or QA?
QC usually determined during mix design.

## Slide 147: Answer – M8 – Q1; (slide 54, 55)
-How applied:
The difference between the measured and the actual % binder is the Asphalt binder Cf.

## Slide 148: Module 8
2. For the Thermolyne brand oven, what is the “Temperature compensation”?
What?
How is it applied?

## Slide 149: Answer – M8 – Q2; (slide 66)
-What is the “Temperature compensation”? Apparent loss in weight due to heating = TCF
How is it applied? Taken off the oven print out if weighed in the oven.
Subtracted from total loss.

## Slide 150: Module 8
3. What is the “Chamber Set Point”? Who decides which of the standard values should be used?
What?
Who decides (QC or QA)?

## Slide 151: Answer – M8 – Q3; (slide 58)
- What is the set point: 538C, High Cf’s (>1.0%): 482 C
Very High Cf’s 427C
Who decides (QC or QA)?
QC

## Slide 152: Module 8
4. On the accompanying “calibration” data sheet, calculate the Asphalt Binder Correction Factor [Aggregate Correction” Factor] (Cf). Assume that the moisture content of the [ab-produced mix is zero. All weighting steps will be performed on an exterior scale.
5. On the accompanying “HMA Moisture Correction” data sheet, calculate moisture content of a plant-produced HMA sample.

## Slide 153: Module 8
6. On the accompanying HMA Asphalt Content (NCAT oven method) data sheet. (“Reproducing Oven Ticket Values”), record the appropriate information from the oven ticket and calculate the moisture-corrected asphalt content of the plant-produced HMA sample (use the moisture determined in question 5).
Note: oven tape Weight loss = 135.6g
oven tape Temperature compensation (%) = 0.12%
oven tape Calib. Factor (Cf) = 0.98%

## Slide 154: Module 8
7. Something happens during an ignition oven test, and you must finish the test manually. You obtain the [Final mass of basket + burned specimen] by weighing on your bench balance. Previous information about this specimen is that there was 0.1% moisture in it, and the aggregate correction factor for the mix is 0.98%. On the accompanying form (Manual Weighing Method”), calculate the binder content.

## Slide 155: Answer – M8 – Q4 to Q7; (slide 57)
M1 = 5.40 – 5.01 = 0.39
M2 = 5.35 – 5.02 = 0.33
M1 = (81/1500) x 100 = 5.40
M2 = (79.2/1480) x 100 = 5.35
M1 = 4500 – 3000 = 1500
M2 = 4480 – 3000 = 1480
Use Regular Rounding

## Slide 156: Answer – M8 – Q4 to Q7;
Use Regular Rounding

## Slide 157: Answer – M8 – Q4 to Q6;
Use Regular Rounding

## Slide 158: Answer – M8 – Q4 to Q7;
Use Regular Rounding

## Slide 159: Module 8
8. At what point is the moisture content determined, during mix design or during field sampling? Who determines the moisture content, QC or QA? How is the moisture correction applied?
When determined:
Who (QC or QA):
How used:
8. If the Aggregate Correction Factor exceeds 1.0% at 482 C, MoDOT specs dictate that the Chamber Set Point (Ignition temperature) should be _______?

## Slide 160: Answer – M8 – Q8, Q8; (slide 58)
8. At what point is the moisture content determined, during mix design or during field sampling? Who determines the moisture content, QC or QA?
How is the moisture correction applied?
When determined: Field Sample
Who (QC or QA): QC or QA
How used: Subtract from apparent binder content (Total Loss)
8. If the Aggregate Correction Factor exceeds 1.0% at 482°C, MoDOT specs dictate that the Chamber Set Point (Ignition temperature) should be __482 ° C_____?

## Slide 161: Module 8
9. If the Aggregate Correction Factor exceeds 1.0% at 482 C, MoDOT specs dictate that the Chamber Set Point (Ignition temperature) should be ______ ?
Answer – (slide 58)
427 °C

## Slide 162: Module 8
10. What test method is specified for moisture determination of hot mix samples?
AASHTO T 329
ANSWER (SLIDE 47):

## Slide 163: Module 8
11. Is it allowable to use the residue of an ignition oven test for gradation analysis?
YES
ANSWER (SLIDE 987):

## Slide 164: Module 8
12. What may be necessary to determine if you were going to use an Ignition oven sample for gradation purposes?
ANSWER (Slide 98)
Aggregate (gradation) Correction Factor

## Slide 165: Module 8
13. What is the QC testing frequency of RAP binder content?
ANSWER (Slide 95)
1 per 4 Sublots

## Slide 166: Module 8
14. What is the QA testing
frequency of RAP binder content?
ANSWER (Slide 95)
1 per project

## Slide 167: Module 8
15. What testing method for RAT binder is specified?
ANSWER (Slide 95)
T164 Solvent Extraction

## Slide 168: Module 8
16. Under what conditions can a different RAP binder content test method be substituted?
ANSWER (Slide 95)
T308 (Ignition Oven) if a correction factor is determined which is the difference between T164 Solvent Extraction and T308 Ignition Burn off.

## Slide 169: Module 8
17. What is the frequency of oven verification?
ANSWER (Slide 106)
Yearly and after each move.

## Slide 170: Module 9 tensile strength ratio (tsr)
1. What should be the finished height of the TSR puck?
ANSWER - (Slide 57)
95 ± 5 mm tall

## Slide 171: Module 9
2. What should be the finished air void content of the TSR puck?
ANSWER (Slide 57)
7.0 ± 0.5%
(SMA 6.0%)

## Slide 172: Module 9
3. What should be the finished % saturation of the TSR puck?

## Slide 173: Module 9
3. What should you do if the core is high on saturation?

## Slide 174: Module 9
4. If the TSR (during production is 72, what is the pay adjustment factor?

## Slide 175: Module 9
4. If the TSR (during production is 72, what is the pay adjustment factor?
ANSWER - (Slide 19)
98 %

## Slide 176: Module 9
5. Under what conditions is TSR required for BP and BB mixes?

## Slide 177: Module 9
6. List some things that might happen which would cause the lab running the TSR to call for more sample?
ANSWER (Slides 64, 65)

## Slide 178: Module 10A Quality Level Analysis – pay factors
1. The Pay Factors for a 4000 ton lot of material placed on the traveled way are as follows. Compute the overall pay factor for this lot:
If the contract unit price per ton of hotmix is $65.00, calculate the bonus or deduct for this lot:

## Slide 179
ANSWER – M10A Q1; (SLIDE 13, 6)
99.6/100 = 0.996

## Slide 180: Module 10A

## Slide 181: Module 10A
3. During HMA production, what are the specification limits (with field tolerances applied) for:
ANSWER (Slide 3)

## Slide 182: Module 10B Quality Level Analysis – Favorable & unfavorable comparison
1. How close must the QA results be to the mean of the QC results in order for the data from QC be considered valid so that the QC results can be used to compute pay factors?
Rule#1:
Rule#2:

## Slide 183: Answer – M10B – Q1; (slide 4)
Rule#1:
Within 2 standard deviations
Rule#2:
Within ½ of the specification tolerance

## Slide 184: Module 10B
2. If QC’s mean binder content is 5.80% with a standard deviation of 0.20% and QA’s binder content is 5.67%, is there favorable comparison?
Note: You will need slide 3 from Module 10A to answer this question.

## Slide 185: Answer – M10B – Q2; (slide 3 from M10a and slide 4 from m10b)
0.20 is standard deviation given in the question
0.3 is from Spec limits chart

## Slide 186: Module 10B
3. If QC’s mean binder content is 5.80% with a standard deviation of 0.50% and QA’s binder content is 5.67%, is there favorable comparison?
Note: Again, you will need slide 3 from Module 10A to answer this question.

## Slide 187: Answer – M10B – Q2; (slide 3 from M10a and slide 4 from m10b)
0.50 is standard deviation given in the question
0.3 is from Spec limits chart

## Slide 188: Module 10B
4. If there is unfavorable comparison between QC and QA, to resolve the issue, what is the first step?
Answer (slide 20)

## Slide 189: Module 10B
5. If all data appears to be correct, what 2 alternate courses of action could be taken?

## Slide 190: Module 10B
6. If a retained sample is tested, what tests must be run?
Answer (slide 23)
Gmm, Gmb, Pb

## Slide 191: Module 10B
7. What constitutes favorable comparison between the 2 original and retained sample test results?
Answer – (slide 24)
Gmm within 0.005
Gmb within 0.010
Pb with in 0.1%

## Slide 192: Module 10B
8. If there is favorable comparison between the original and retained sample test results, what should be done?
Answer – (slide 24)
Use original in data set and add QA’s results.
Rerun the PWL Analysis

## Slide 193: Module 10B
9. If there is un-favorable comparison between the original and retained sample test results, what should be done?
Answer – (slide 26)
Substitute (Pb, Gmm, Gmb) results from retained
Split, re-calculate Va and VMA.

## Slide 194: Module 10B
10. If the retained sample test results are substituted for original results and the lot comparison still shows unfavorable comparison between QC and QA, what should be done?
Answer – (slide 26)
Add in QA’s Results
Rerun PWL Analysis.

## Slide 195: Module 10C Quality Level Analysis – Miscellaneous
Under what circumstances would material be considered for removal & replacement?

## Slide 196
ANSWER – M10C - Q1; (SLIDE 17)
PF < 50.0
TSR < 65%
Air Voids < 2.5%
Any sub-lot with < 90.0 or >98% density
Unconfined joint density < 88.0% or
> 98.0%

## Slide 197: Module 10C
2. The payment for non-integral should lots can also be adjusted for Density by use of the Density pay adjustment Table.
Answer – (slide 13)

## Slide 198: Module 10D Quality Level Analysis – Performance Testing
1. What are the two performance tests currently being explored through JSP’s?
Answer – (slide 3)
Fatigue cracking – FI or Ideal CT
Rutting – Hamburg Wheel Tracker

## Slide 199: Module 11 Record keeping & exchange of data
1. What lab equipment calibration records must be kept?
Answer – (slide 6)

## Slide 200: Module 11
2. A record of certain information must be kept 3 years. List the types of required information.
Answer – (slide 9)

## Slide 201: Module 11
3. In regard to test data and results, when should QC make it available to QA and what info is required?
Answer – (slide 10)

## Slide 202: Module 11
4. In regard to test data and results, when should QA make it available to QC and what info is required?
Answer – (slide 10)
Not later than the beginning of the next workday.
Raw data including Gyros and Binder printouts

## Slide 203: Module 11
5. List some things that a process review team may ask for.
Answer – (slide 3,4,5,6)

## Slide 204: Module 12 contract administration
Are MoDOT inspectors limited to taking only random HMA samples off the roadway?
Answer – No – Can take check samples
Under what conditions can self-test results be used for determining removal limits?
Answer – Gyro and Binder Printouts, Well documented

## Slide 205: THE END
09/10/2021